Supporting information

Direct Silicon Heterostructures with Methylammonium Lead Iodide Perovskite for Photovoltaic Applications

IEEE Journal of Photovoltaics doi 10.1109/JPHOTOV.2020.2981805

Authors

Silvia Mariotti1,5*, Mohammed Al Turkestani2, Oliver S. Hutter1, Georgios Papageorgiou1,3, Jonathan D. Major1, Jack Swallow1, Pabitra K. Nayak4, Henry J. Snaith4, Vinod R. Dhanak1, Ken Durose1

Affiliation:

1 Stephenson Institute for Renewable Energy / Department of Physics, University of Liverpool, Peach St, Liverpool, L69 7ZF, United Kingdom

2 Department of Physics, Umm Al-Qura University, Makkah, Saudi Arabia

3 Now at: CTF Solar, Zur Wetterwarte 50, Haus 303, 01109 Dresden, Germany

4 Department of Physics, Clarendon Laboratory, Department of Physics, University of Oxford, Oxford, UK

5 Now at: Laboratoire de Chimie des Polymères Organiques, LCPO UMR 5629 CNRS, Université de Bordeaux, Bordeaux INP, Allée Geoffroy Saint-Hilaire, B8, F-33615 Pessac, Cedex, France.

*E-mail: silvia.mariotti@u-bordeaux.fr

Device fabrication

n-Si wafers were cut to 2 x 1 cm and cleaned with the RCA procedure: the silicon pieces were soaked in acetone at 35°C for 10 min and then soaked in methanol for 5 min. After rinsing with water and drying with nitrogen, wafers were soaked for 15 min in a H2O2 : NH4OH solution in DI water (1:1:5 by volume respectively), which was previously boiled at 70°C until it showed distinct bubbling for 1-2 minutes. The samples were then rinsed with large amounts of water and dried. In an appropriate water-flushed fume hood, a 2% HF solution was prepared and the silicon was soaked in the solution for 2 minutes and then rinsed with running water. (The effectiveness of the HF treatment was checked with an hydrophobicity test: effective SiO2 removal yields surfaces that reject water droplets). Immediately after this process, the wafers were transferred into a nitrogen glovebox and a filtered solution of lead iodide/methylammonium iodide/DMSO (1:1:1 molar ratio) in 0.6 ml DMF,  was dynamically spin-coated onto the silicon (50 μl, 4000 rpm, 25 sec) and then annealed at 60°C for 1 min and 100°C.

Spiro-OMeTAD (2,2',7,7'-tetrakis-(N,N-di-4-methoxyphenylamino)-9,9'-spirobifluorene) was used as a hole transporting material and was deposited on top of the perovskite layer. A solution of spiro-OMeTAD  in chlorobenzene and doped with Li-bis-sulfonamide solution in acetonitrile and 4-tert-butyl pyridine, was spin-coated on MAPI’s surface, at 3000 rpm for 30 seconds. Samples were then kept in the dark in a desiccator over night to oxidise the spiro-OMeTAD layer which then became conductive.

A very thin layer (10 nm) of gold was then thermally evaporated on the whole surface, while thin lines of gold (1 mm width, 50 nm thick) were deposited to prepare the contacts. After scratching off the perovskite and the spiro-OMeTAD on a small edge of the device, aluminium was deposited onto the silicon to form the back contact. The cell was finally scribed to have contact areas of 0.15 cm2 and then measured.

Contacts to organic layers in test structures

Figure S1:  In order to test for the Ohmic or rectifying nature of the organic films test structures on glass were formed, in which a pre-deposited metallic film was part coated with the organic, in this case MAPI. This allowed contacting to both sides of the organic film.

Characterisation

- Perovskite characterisation

Films grown on silicon were analysed with X-ray diffractometer (X’Pert PRO X-ray diffraction system – Philips Analytical, using a Cu X-ray tube).

MAPI films prepared on glass were analysed with a spectrophotometer (SolidSpec-3700 UV-VIS-NIR Spectrophotometer – Shimadzu) measuring transmittance and reflectance spectra, which were converted to absorption coefficient spectra and Tauc plots for direct gap semiconductor (Fig. S1a, b, c).

X-ray photoelectron spectroscopy (XPS) was also used to determine the position of the Fermi level relative to the valence band. The analyses, shown in Fig. S2c and d, present a band gap of 1.57 eV – in accordance to the expected band gap for MAPI – and a valence band energy maximum (EVBM) of 0.89 eV, which corresponds to the energetic gap between the valence band and the Fermi level (positioned at 0 eV). Hence, the position of the Fermi level is in the centre of the band gap within experimental error and therefore we determined that the MAPI synthesised with the procedure presented previously, is intrinsic.

XPS photoemission measurements were performed in a standard ultrahigh vacuum chamber with a base operating pressure of ≈1·10-10 mbar. Samples were mounted to metallic plates and tantalum straps were spot welded to the plates contacting the sample surface to minimise charging under illumination. X-ray photoemission spectroscopy was performed using a PSP Vacuum Technology Al Kα X-ray source (hv = 1486.6 eV) operating at 144 W, with a PSP electron-energy analyser operating at a pass energy of 20 eV. Samples were measured as entered, and a small charge correction was applied to spectra using the C1s (284.8 eV) as the reference peak.

Fig. S2. Optical measurements of MAPI thin films grown on glass. a) Transmittance (black circles) and reflectance (blue triangles) of a 300 nm MAPI film. b) Absorption coefficient of MAPI, derived from data in a). c) Tauc plot of MAPI calculated as a direct semiconductor and extrapolated from the absorption coefficient measured on the film via spectrophotometric analysis (transmittance and reflectance), giving a 1.57 eV band-gap. d) XPS measurement of a MAPI film deposited on molybdenum foil, showing a difference of 0.89 eV between the valence band edge and the Fermi level (at 0 eV). Since the band-gap is known from the Tauc plot, it can be concluded that the perovskite layer is intrinsic, within the experimental error.

- Device characterisation

Devices were examined with SEM (JEOL JSM-7001F), a solar simulator (TS Space Systems, calibrated at AM 1.5 (100 mW/cm2) using a scan rate of 0.19 V/s), an EQE (Bentham PVE300, operating with a 0.75mm square slit) and C-V kit (Solartron, 1260 Impedance/Gain-phase analyser combined to 1296 Dielectric interface).

Au, spiro-OMeTAD and spiro-OMeTAD/Au optical behaviours

Fig. S3.  These transmittance measurements were performed on films deposited on glass, i.e. glass/Au (10 nm) (black), glass/spiro-OMeTAD (blue) and glass/spiro-OMeTAD/Au (10 nm) (red).

The transmittance decreases when on pure spiro-OMeTAD (blue) a 10 nm layer of Au is deposited (red). However, pure Au (black) transmittance increases when the Au is deposited onto spiro-OMeTAD (red), allowing more light in the device. Hence, adding a layer of spiro-OMeTAD in the n-Si/MAPI/Au devices may optically benefit the device performance.

Capacitance-Voltage analysis

The depletion region capacitance is:

C= dQdV

The total depletion width is calculated as the sum of the widths in both semiconductors involved in the junction (w1 and w2):

W= w1+w2

The Mott Schottky plot, a graph showing 1/C2 versus voltage, is a useful tool to extrapolate built in voltage Vbi and carrier concentration N, however it is important to know if the junction is a one-sided or a two-sided in order to avoid misinterpretation: while the built in voltages are directly extracted from the Mott-Schottky plot, the determination of the carrier concentration is dependent on the dielectric constant of the materials involved in the junction (only one dielectric constant for one-sided junctions and two dielectric constants for two-sided junctions).

For one-sided junctions:

W is calculated as (*): W=εrε0AC

Hence in the Mott-Schottky plot (*): 1C2=2 VbiA2eεrε0N-2 VA2eεrε0N

From the fitting of the Mott-Schottky plot (having formula y = mx + b), it is possible to derive (*):   Vbi=-bm+TkBe   and   N=2m A2eεrε0

* Where: W is the width of the depletion region, C is capacitance, εr is the dielectric constant of the semiconductor containing the depletion region, ε0 is the permittivity in free space, A is the contact area, Vbi is the built in voltage, e is the electron charge, T is temperature, kB is Boltzmann’s constant, N is the carrier concentration of the semiconductor containing the depletion region.

For two-sided junctions:

The capacitance is dependent to the dielectric constant, hence: C1= εr1ε0Aω/2 and C2= εr2ε0Aω/2

Which may be simplified as: C= ε Aω

where: ε= 2εr1εr2ε0 (εr1+εr2)

W (under applied bias) is calculated as(*): W=2ε(Vbi-V)e Na+NdNaNd

Hence in the Mott-Schottky plot(*): 1C2= 4 VbiA22eεNa+NdNaNd- 4 VA22eεNa+NdNaNd

- And by knowing “b” from the fitting in the Mott-Schottky plot (having formula y = mx + b), Na may be determined as follows(*): Na= 4 VbiNd bA22eεNd-4 Vbi

* Where: Na is the acceptor carrier concentration, Nd is the donor carrier concentration, εr1 is the dielectric constant of one semiconductor, εr2 is the dielectric constant of second semiconductor, ε is the dielectric constant of the junction.

The carrier concentration unit is cm-3.

|  |  |  | C – V device results |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  |  | One-sided junction | Two-sided junction |  |
| - Si resistivity | Vbi (V) | Manufacturer’s n-Si carrier concentration (cm-3) | n-Si carrier concentration (cm-3) | n-Si carrier concentration (cm-3) | MAPI carrier concentration (cm-3) |
| - 1-5 Ω·cm | # 0.70 ± 0.01 | # 2.86 x 1015 | # 1.39 x 1015 | # 1.03 x 1015 | # 1.62 x 1015 |
| - 5-10 Ω·cm | # 0.68 ± 0.01 | # 6.68 x 1014 | # 7.90 x 1014 | # 5.87 x 1014 | # 7.58 x 1015 |
| - 10-15 Ω·cm | # 0.65 ± 0.01 | # 3.67 x 1014 | # 3.28 x 1014 | # 2.44 x 1014 | # 8.30 x 1014 |

Table S1. Results from C-V analysis performed on Al/n-Si/MAPI/spiro-OMeTAD/Au devices using Si wafers with different resistivities. The carrier concentrations obtained using both the one- and two-sided junction approximations are shown.

Band diagram

In order to produce the band offset shown in Fig. 6, this band alignment (before equilibrium) was used.

Fig. S4. a) Band energies of the Al/n-Si/MAPI/spiro-OMeTAD/Au device materials before equilibrium. Band energies were taken from ref. 19 and 20 (see main manuscript). b) Equilibrium band diagrams for an Al/n-Si/MAPI/spiro-OMeTAD/Au device, considering a one-sided junction with the field in the MAPI and using n-Si with low doping.