## Slide 1
Topography of octanedioic-acid & nonanedioic-aicd pεK gels
AFM images demonstrating the topography of pεK hydrogel variants. PεK (0.07g/ml. 0.1g/ml or 0.13g/ml) was cross-linked 60% with either octanedioic-acid or nonanedioic-acid. AFM micrographs illustrate that increasing the amount of pεK within the gel changes the open porous structure to a tighter close knit structure. Height range 5nm – -5nm.
IV) 60-0.07-Non
V) 60-0.1-Non
I) 60-0.07-Oct
II) 60-0.1-Oct
III) 60-0.13-Oct
VI) 60-0.13-Non