Research data for paper entitled “Insights into post-growth doping and proposals for CdTe:In photovoltaic devices”

The paper has been submitted to IoP J Phys: Energy in 2022.

This deposit constitutes the research data included in the paper. The majority of the data is in the form of graphs for which the original data is contained in Origin files labeled with the name of the figure to which they pertain. For the photoemission data, the original data is included in a zip file named ‘photoemission data’.

Insights into post-growth doping and proposals for CdTe:In photovoltaic devices

Luke Thomas1, Theo D.C. Hobson1, Laurie J. Phillips1, Kieran J. Cheetham1, 2, Neil Tarbuck1, Leanne A. H. Jones1. Matt J. Smiles1, Chris H. Don1, Pardeep K. Thakur3, Mark Isaacs4, Huw Shiel1,5, Stephen Campbell6, Vincent Barrioz6, Vin Dhanak1, Tim Veal1. Jonathan D. Major1 and Ken Durose*1

1 – Dept. Physics/Stephenson Inst for Renewable Energy, Univ. Liverpool, L69 7ZF, UK

2 – Now at: STFC, Daresbury Laboratory, Keckwick Lane, Daresbury, Cheshire, WA4 4AD, UK

3 – Diamond Light Source, Harwell Science & Innovation Campus, Didcot, Oxfordshire, OX11 0DE, UK

4 – Harwell XPS, Research Complex at Harwell (RCaH), Didcot, OX11 0FA, UK

5 – Now at: Dept. of Materials, Imperial College London, Prince Consort Road, London, SW7 2BP, UK

6 – Dept Maths, Physics and Elect. Eng, Univ Northumbria, Newcastle-upon-Tyne, NE1 8ST, UK

KEYWORDS: Thin film solar cell; photovoltaics; cadmium telluride; n-type absorber; doping; indium

Abstract.

This paper is motivated by the potential advantages of higher doping and lower contact barriers in CdTe photovoltaic devices that may be realized by using n- type rather than the conventional p-type solar absorber layers. We present post-growth doping trials for indium in thin polycrystalline CdTe films using diffusion of indium metal and with indium chloride. Chemical concentrations of indium up to 1019 cm-3 were achieved and the films were verified as n-type by hard x-ray photoemission. Post-growth chlorine treatment (or InCl3) was found to compensate the n-doping. Trial structures comprising CdS/CdTe:In verified that the doped absorber structures performed as expected both before and after chloride treatment, but it is recognized that this is not an optimum combination. Hence in order to identify how the advantages of n-type absorbers might be fully realized in future work, we also report simulations of a range of p-n junction combinations with n-CdTe, a number of which have the potential for high Voc.